## Slide 1: Strength analysis of laminates with circular cutouts under tension
Zheng Li, Jianlin Chen, Pengcheng Chu
State Key Laboratory for Turbulence and Complex Systems, Department of Mechanics and Engineering Science, College of Engineering, Peking University, China

## Slide 2: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 3: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 4: 1. Introduction (i)
Composite Structures with Big Cutout inevitably
Aircraft
Notes: .

## Slide 5: 1. Introduction (ii)
How to predict the failure of laminates with big cutouts？
S.T. Pinho COMPOS: Part A, 2006(37)
Ireneusz L. COMPOS: Part A, 2007(38)
P. Maimı´ MECH MATER, 2007(39)
Chi-Seung Lee COMPOS STRUCT, 2015(121)

## Slide 6: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 7: 2. Simulation (i)
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1781.1 | 1160 | 36.8 | 182 | 88
Table 2 Strength parameters of a single lamina (T700/9363)
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 130.40 | 7.12 | 3.80 | 0.274
Table 1 Material properties of a single lamina (T700/9363)
FEM：Abaqus software
Model: 3D Shell SC8R
Strength criterion：Hashin
FEM Model
Ф: 60mm, 80mm, 100mm
Layups: [0˚]8, [0˚/90˚]2S, [±45˚]2S
1: Failure mode
2: Ultimate load

## Slide 8: 2. Simulation (ii)
The definition for the ply complementary free energy density:
The lamina compliance tensor:
The strain tensor:
P. Maimí, P.P. Camanho, J.A. Mayugo, et al. A continuum damage model for composite laminates: Part I – Constitutive model[J]. Mechanics of Materials, 2007, 39:897–908.
Inverse matrix is the stiffness tensor:
Constitutive damage model:
Notes: To establish a constitutive law, it is possible to define a scalar function corresponding to the complementary free energy density in the material.The proposed definition for the ply complementary free energy density is:
The damage variables as a measure of the effective surface density of the microdefects.
The strain tensor is equal to the derivative of the complementary free energy density with respect to the stress tensor:

## Slide 9: 2. Simulation (iii)
Hashin criterion
Damage variable
Continuum Damage Model:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Damage Model
Notes: In the failure simulation, we use the Hashin criterion to determine the crack’s happening, and then use the linear continuum damage model to simulate the crack’s propagation.

## Slide 10: 2. Simulation (iv)
Damage variables calculation：
damage variables:
Jacobian matirx:
Notes: 在传统强度理论研究中，通常将单向板试验获得的拉伸、压缩和剪切强度值作为材料的固有属性并用于建立强度准则，进而预测多向层合板的强度。然而通过一系列试验研究发现，对于铺层方向和厚度都相同的子层，它在多向层合板内和在单向板内时表现出的基体强度（包括横向拉伸和剪切强度）不同，在层合板内表现的强度明显高于在单向板内，许多文献将层合板的这种现象称为就地效应（in-situ effect）。
By examining the results presented previously,5±7 we take the in-situ tensile transverse and shear strengths to be 1.5 times those measured from unidirectional laminates for all the laminates discussed.

## Slide 11: 2. Simulation (v)
Damage variable:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Damage variable:
Damage and Failure Study of Composite Laminates with
Reinforced Cutout Based on CDM
Wang Wenzhi，Wan Xiaopeng，Yao Liaojun
Exponential degenaration:
Linear degenaration:
Maimí P, Camanho P P, Mayugo J A, et al. A continuum damage model for composite laminates: Part II – Computational implementation and validation[J]. Mechanics of Materials, 2007, 39(10):909–919.
Notes: 基于不可逆过程的热力学，将势能定义为损伤变量的函数，损伤变量定义了应力应变的关系，同时取决于能量耗散值
所有使用参数均可测量得到
可以模拟材料的弹脆性行为
可以计算层合板的损伤演化过程
在abaqus中使用UMAT子程序实现

## Slide 12: 2. Simulations (vi)
Flowchart of failure process：
calculate strain and undamaged stiffness matrix
calculate damage variable d and
calculate stress and Jacobian matirx; update damage variable d
undamaged
damaged
calculate damaged stiffness matrix
each increment
quit UMAT,back to main program
calculate stress
UMAT subroutine
checkout failure ( Hashin
criterion)
Notes: Here is the flowchart of failure process.

## Slide 13: 2. Simulations (vi)
[0]10 unidirectional-ply & Ф80mm
Fiber failure
Matrix failure
Failure mode and crack propagation
Notes: Here is the simulation results, the failure mode and crack propagation of unidirectional-ply with cutout Phi 80mm. We can see the failure process, each of fiber and matrix. So the matrix failure occurs, but the fiber not break. The total failure mode like this.

## Slide 14: 2. Simulations (vii)
[0/90]5 cross-ply & Ф80mm
Fiber failure
Matrix failure
Fiber failure
Matrix failure
layer
layer
Notes: Also we can see the cross-ply’s results. In the 0 degree layer, the fiber failure and matrix failure both happen. But in the 90 degree layer, just there is the matrix failure. And here is the final crack propagation path.

## Slide 15: 2. Simulations (viii)
[45]5 angle-ply & Ф80mm
Fiber failure
Matrix failure
Notes: In the angle-ply, we can only see the matrix failure.

## Slide 16: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 17: 3. Experiments (i)
DIC speckle (Front side)
Experiment system
Cutouts: (a) Ф60mm (b) Ф80mm (c) Ф100mm
Layup sequences
unidirection-ply
cross-ply
Loading mode
Displacement control by 0.5mm/min
3D Digital Image Correlation (DIC) test
PMBLAB DIC-3D system Pro
Camera: 2448*2048pix
Images: 1f/kN
Correlation algorithms: ZNSSD
Strain gauges sketch
Notes: Here is the experiment system. We use strain gauges and 3 dimension digital image correlation method to measure the strain. Here is DIC speckle. We also consider 4 types of layup and 3 sizes of cutout.

## Slide 18: 3. Experiments (ii)
Strain comparison between strain gauges, DIC and simulation results
Strain
Gauges
DIC
Test points
- Ф60mm
Notes: In the experiment, we compare the strain results between the gauges, DIC and simulation. Here are the strain testing points. The 3 results are in good agreement. So the DIC testing method is ok.

## Slide 19: 3. Experiments (iii)
Load-Displacement Curves
Ф60
Ф80
Ф100
The failure process is like a brittle fracture
ε1
ε1
-H80
-H80
Notes: Here are load-displacement curves. The curves go straight up, and drop down at last. So the failure process is like a brittle fracture.
In the unidirectional-ply loading curve, we find that there are some little drop down points. It means the cracks occur. The DIC results can show that. But in the other layup specimens, we can’t see this situation.

## Slide 20: 3. Experiments (iv)
v
in Cutout Ф80mm by DIC at 10kN
Strain εx
Strain/Stress concentration
x
y
SCF results
by Exp.
60 80 100
Notes: According to the strain epsilon x results, we can see the strain/stress concentration happen.
And here are the stress concentration factor results by strain gauges testing. It shows that the cutouts bigger, the stress concentration factors larger.

## Slide 21: 3. Experiments (v)
Failure Modes
（cracks along ）
（cracks along ）
（cracks along ）
Ultimate loads
60 80 100
Notes: Here are the failure modes of each layup specimens. In the unidirectional-ply, the cracks propagation along the 0 degree. In the cross-ply, the cracks along the 90 degree.
In the angle-ply, the cracks along the 45 degree. In the quasi-isotropic-ply, the cracks along the 90 and 45 degree, depend on the layers. We also calculate the total failure loads or the final strength loads. The unidirectional-ply, the black bars, can support the highest loads, and the angle-ply, the blue bars, the lowest.

## Slide 22: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 23: 4. Results and discussion (i)
[0]10
Linear degenaration
Exponential degenaration
60mm
80mm
100mm
Failure evolution：

## Slide 24: 4. Results and discussion (ii)
60mm
80mm
100mm
0 ply
90 ply
fiber
fiber
matrix
matrix
[0/90]5
Failure evolution：Exponential degenaration

## Slide 25: 4. Results and discussion (iii)
[0/90]5 | 60 |  |  | 80 |  |  | 100 |  | 
 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
Linear | 52.67 | 59.32 | 11.2% | 43.83 | 47.20 | 7.1% | 34.56 | 37.54 | 7.9%
Exponential | 56.72 |  | 4.4% | 48.17 |  | 2.1% | 34.59 |  | 7.9%
[0/90]5
Ultimate loading：
Simulation
Experiment
Notes: 1、从试验以及模拟的结果来看，裂纹的扩展和孔径大小无关，孔径越小，极限载荷越大
2、计算结果可以表现出[0/90]5板的脆性断裂，
3、linear或是exponential模型对损伤演化的影响不太大，exponential比linear计算极限载荷的误差更小

## Slide 26: 4. Results and discussion (iv)
60mm
80mm
100mm
Linear degenaration
Exponential degenaration
[±45]5
Failure evolution：

## Slide 27: 4. Results and discussion (v)
 | 60 |  |  | 80 |  |  | 100 |  | 
[±45]5 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
Linear | 21.41 | 28.72 | 25.5% | 17.03 | 23.79 | 28.4% | 12.75 | 17.60 | 27.6%
Exp. | 27.34 |  | 4.8% | 21.73 |  | 8.7% | 16.09 |  | 8.6%
[±45]5
Ultimate loading：
Simulation
Experiment
Notes: 1、从试验以及模拟的结果来看，裂纹的扩展和孔径大小无关，孔径越小，极限载荷越大
2、linear或是exponential模型对损伤演化的影响不太大，极限载荷：exponential比linear误差更小
4、位移载荷曲线的形状和实验相差大

## Slide 28: 4. Results and discussion (vi)
Shear Nonlinearity:
Shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
n is a parameter define the shape of the nonlinear stress-strain relationship.
The displacement-load curve is closer to the experiment when n=2.

## Slide 29: 4. Results and discussion (vii)
Shear Nonlinearity:
Experiment
N=2
No Shear Nonlinearity
Problem:The load of the curve doesn't drop in the simulation result.

## Slide 30: 4. Results and discussion (viii)
 | 60 |  |  | 80 |  |  | 100 |  | 
[±45]5 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
No shear nonlinearity | 27.34 | 28.72 | 4.8% | 21.73 | 23.79 | 8.7% | 16.09 | 17.60 | 8.6%
Shear nonlinearity | 26.81 |  | 6.7% | 21.39 |  | 10.1% | 16.01 |  | 9.0%

## Slide 31: Contents
Introduction
1
2
3
5
Numerical Simulations
Experiments
Conclusions
4
Results and discussion

## Slide 32: 5. Conclusions
Failure process is a typical brittle fracture;
Failure onset is at the stress concentration area, ultimate strength is effected by the design of ply sequences and decreases with the size of cutout increase
The failure evolution of laminates doesn't affected by the size of cutout, and the failure of each single layer always includes different failure modes.
The continuum damage model preforms well for predicting the failure evolution behavior of composite laminates with big cutouts. The shear nonlinearity must be considered for the [±45]5 layup laminates.

## Slide 33: Acknowledgement
Project supported by the National Natural Science
Foundation of China (No. 11232001)
Thank you for your attention
Zheng Li
Email: lizheng@pku.edu.cn