## Slide 1
Content：
the model and the method
compare two different degeneration model(linear vs exponential)
conclusion and discussion

## Slide 2
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1518 | 764.3 | 36.0 | 160.3 | 60
Table 2 Strength parameters of a single lamina
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 127.70 | 9.67 | 6.50 | 0.30
Table 1 Material properties of a single lamina
FEM：Abaqus
Model: 3D Shell(SC8R)
Strength criterion：Hashin
Simulation Model
Ф: 60mm, 80mm, 100mm
Layups: [0˚]10, [0˚/90˚]5, [±45˚]5

## Slide 3
Ply-discount model:
Hashin criterion
Wang Danyong, Wen Weidong, Cui Haitao. Three-Dimensional progressive damage analysis of composite laminates containing a hole subjected to tensile loading. Chinese Journal of Theoretical and Applied Mechanics, 2005, 37(6):788-795.
Ply-discount model
Simulation Model

## Slide 4
Damage variable:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Continuum Damage Model I（Linear degenaration law)
）
Simulation Model

## Slide 5
Damage variable:
Damage and Failure Study of Composite Laminates with
Reinforced Cutout Based on CDM
Wang Wenzhi，Wan Xiaopeng，Yao Liaojun
Continuum Damage Model II（Exponential degenaration law)
Simulation Model

## Slide 6
calculate strain and undamaged stiffness matrix
calculate damage variable d and
calculate stress and Jacobian matrix; update damage variable d
damaged
undamaged
calculate damaged stiffness matrix
after each increment
quit UMAT,back to main program
calculate stress
UMAT subroutine
checkout failure ( Hashin
criterion)
UMAT subroutine：

## Slide 7
Ultimate load （kN） Layer | Exp. | Linear degenaration | 
 |  | Simulation | Error
[0]10 | 69.73 | 86.98 | 24.73%
[0/90]5 | 47.20 | 45.37 | 3.88%
[±45]5 | 23.79 | 14.31 | 39.85%
The ultimate strength:
Linear degenaration
Experiment
Exponential degenaration | 
Simulation | Error
87.32 | 25.23%
50.67 | 7.35%
15.04 | 36.78%
Exponential degenaration
Results and Comparing

## Slide 8
[0]10
Fiber failure
Matrix failure
Matrix failure
Fiber failure
Linear degenaration
Exponential degenaration
Results and Comparing

## Slide 9
[0/90]5
Fiber failure
Matrix failure
layer
layer
Linear degenaration
Exponential degenaration
Results and Comparing
Notes: This is the failure behavior of the 0/90 layup laminates. The fiber failure is shown in the animation above. The matrix failure is shown in the animation below,The left one is 0 layer,the right one is 90 layer. In the 0 layer,we can see that the fiber failure extends along the 90 direction,and the matrix failure also extends on the either sides of the fiber failure.In the 90 layer,there is only matrix failure without any fiber failure.

## Slide 10
Fiber failure
Matrix failure
[±45]5
Linear degenaration
Exponential degenaration
Fiber failure
Matrix failure
Results and Comparing
Notes: This is the failure behavior of the 45 layup laminates.The matrix failure extends along the 45 direction.The simulation agree with the experimental results.

## Slide 11
Results and Comparing
S12 = 65
Experiment
S12 = 95
Influence of the shear strength S12 ：

## Slide 12
The continuum damage models using the exponential degenaration law and the linear degenaration law almost have same preformance for predicting the failure behavior and the ultimate strength of composite laminates with big cutouts;
The simulation using the exponential degenaration law has an affect on the displacement-force curve in the [±45]5 layup laminates but still did not agree well with the expriment.
next step:
1. cohesive element
2. shear nonlinearity
Conclusions