## Slide 1
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1518 | 764.3 | 36.0 | 160.3 | 60
Table 2 Strength parameters of a single lamina
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 127.70 | 9.67 | 6.50 | 0.30
Table 1 Material properties of a single lamina
FEM：Abaqus
Model: 3D Shell(SC8R)
Strength criterion：Hashin
Simulation Model
Ф: 60mm, 80mm, 100mm
Layups: [0˚]10, [0˚/90˚]5, [±45˚]5

## Slide 2
Shear Nonlinearity：
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
刘魏光, 余音, 汪海. 考虑剪切非线性的复合材料渐进损伤模型[J]. 上海交通大学学报, 2016, 50(2):194-199.

## Slide 3
Ultimate load （kN） Layer | Exp. | Linear degenaration | 
 |  | Simulation | Error
[0]10 | 69.73 | 86.98 | 24.73%
[0/90]5 | 47.20 | 45.37 | 3.88%
[±45]5 | 23.79 | 14.31 | 39.85%
The ultimate strength:
Linear degenaration
Experiment
Exponential degenaration | 
Simulation | Error
87.32 | 25.23%
50.67 | 7.35%
15.04 | 36.78%
Exponential degenaration
Former Results：

## Slide 4
calculate strain and undamaged stiffness matrix
calculate damage variable d and
calculate stress and Jacobian matrix; update damage variable d
damaged
undamaged
calculate damaged stiffness matrix
after each increment
quit UMAT,back to main program
calculate stress
UMAT subroutine
checkout failure ( Hashin
criterion)
UMAT subroutine：

## Slide 5
Experiment
Exponential degenaration
Results and Comparing
Displacement-Force curve of the [45/-45] 5 with different shape parameters.
linear

## Slide 6
Results and Comparing
n = 2 n = 3
experiment
shear nonlinearity:
The position of the initial failure is the same and argrees well with the experiment.

## Slide 7
Improvement
Failure mode with different Fracture energe ：
Refer to other papers:
Gm = 5 Gm = 0.5
A continuum damage model for composite laminates: Part II – Computational implementation and validation
Laminate damage model for composite structures