## Slide 1
Numerical model
Hashin Criteria & Continumm Damage Model(CDM)
Degeneration Model(linear vs exponential)
Shear Nonlinearity
就地强度准测？？
Abaqus simulation
UMAT subroutine
Characteristic Length
coefficient of viscosity
implicit dynamic
Results

## Slide 2
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1518 | 764.3 | 36.0 | 160.3 | 60
Table 2 Strength parameters of a single lamina
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 127.70 | 9.67 | 6.50 | 0.30
Table 1 Material properties of a single lamina
FEM：Abaqus
Model: 3D Shell(SC8R)
Strength criterion：Hashin
Problem：
Ф: 60mm, 80mm, 100mm
Layups: [0˚]10, [0˚/90˚]5, [±45˚]5

## Slide 3
  Numerical Model
  Hashin criteria & Continuum Damage Model
Hashin criterion
Damage variable:
The Continuum Damage Model:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.

## Slide 4
  Numerical Model
  Hashin criteria & Continuum Damage Model
Damage variables calculation：
damage variables:
Jaccobian matirx:

## Slide 5
  Numerical Model
  Degeneration Model(linear vs exponential)
Damage variable:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Damage variable:
Damage and Failure Study of Composite Laminates with
Reinforced Cutout Based on CDM
Wang Wenzhi，Wan Xiaopeng，Yao Liaojun
Exponential degenaration:
Linear degenaration:

## Slide 6
  Numerical Model
  Degeneration Model(linear vs exponential)
Maimí P, Camanho P P, Mayugo J A, et al. A continuum damage model for composite laminates: Part II – Computational implementation and validation[J]. Mechanics of Materials, 2007, 39(10):909–919.
指数损伤演化，损伤变量可写为：
表示阈值，未损伤时为1，损伤后为失效准则的表达式
对能量耗散率进行积分，等于总的能量耗散值（与单元尺寸无关）：
通过以上而是可计算出参数 ，即可得到损伤变量d。

## Slide 7
  Numerical Model—Shear Nonlinearity
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
刘魏光, 余音, 汪海. 考虑剪切非线性的复合材料渐进损伤模型[J]. 上海交通大学学报, 2016, 50(2):194-199.

## Slide 8
  Abaqus Simulation—UMAT subroutine
1 可以用来定义新的材料的本构模型。
2 对于每个增量步，在单元的所有物质点处被调用。
3 在增量步末必须更新应力和状态变量(solution-dependent)
4 必须提供材料的Jocobian矩阵：
UMAT简介：

## Slide 9
  Abaqus Simulation—UMAT subroutine
计算应变，计算未损伤时的刚度矩阵
检查有无损伤
（失效准则）
计算损伤变量d以及
计算应力 计算Jacobian矩阵 更新损伤变量
有损伤
无损伤
计算损伤刚度矩阵
每一增量步调用UMAT子程序
退出UMAT，返回到有限元主程序
损伤变量的表达式：
UMAT
Jaccobian矩阵：

## Slide 10
calculate strain and undamaged stiffness matrix
calculate damage variable d and
calculate stress and Jacobian matrix; update damage variable d
damaged
undamaged
calculate damaged stiffness matrix
after each increment
quit UMAT,back to main program
calculate stress
UMAT subroutine
checkout failure ( Hashin
criterion)
  Abaqus Simulation—UMAT subroutine

## Slide 11
  Abaqus Simulation—Characteristic Length
abaqus内置模型：
1、损伤演化：
为了避免网格依赖性，使用特征长度法，损伤变量的演化会使应力-位移的关系如右图所示
特征长度Lc由单元尺寸，对于壳单元，特征长度为参考平面面积的平方根

## Slide 12
  Abaqus Simulation—Characteristic Length
损伤演化(损伤变量d的演化)取决于：（1）断裂过程中的应变能耗散值（2）应力与应变的软化关系（线性、指数）。
网格依赖性：
在应变软化行为中会导致应变局部化，有限元计算结果会产生网格依赖性，如右图所示，越精细的网格其能量耗散越小。即能量耗散值与失效单元体积成正比。
裂纹带模型：将断裂模拟为一条平行紧密分布的微裂纹带，此时，极限失效应变不再为常数：
特征长度Lc有多种取法，对于壳单元，特征长度为参考平面面积的平方根
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.

## Slide 13
  Abaqus Simulation—coefficient of viscosity
To improve convergence, a technique based on viscous regularization (a generalization of the DuvautLions
regularization) of the damage variables is implemented in the user subroutine. In this technique we do not use the damage variables calculated from the aforementioned damage evolution equations directly; instead, the damage variables are “regularized” via the following equations:
the above equations are discretized in follows:
From the above expressions it can be seen that:
Therefore, the Jacobian matrix can be further formulated as follows:
Care must be exercised to choose an appropriate value for since a large value of viscosity might cause a
noticeable delay in the degradation of the stiffness.
Abaqus Example Problem Manual:Failure of blunt notched fiber metal laminates

## Slide 14
Prediction of size effects in notched laminates using continuum damage mechanics，P.P. Camanho a,*, P. Maimı´ b, C.G. Da´vila ,Composites Science and Technology 67 (2007) 2715–2727
The use of an implicit dynamic finite element model enables the prediction of the load drop that occurs when the specimens fail catastrophically.
implicit dynamic analysis VS static analysis
此处分析步的time period设为60，时间长度越大，越接近脆性。
将密度设为小值，保持不受惯性力的影响
  Abaqus Simulation—implicit dynamic

## Slide 15
Ultimate load （kN） Layer | Exp. | Linear degenaration | 
 |  | Simulation | Error
[0]10 | 69.73 | 86.98 | 24.73%
[0/90]5 | 47.20 | 45.37 | 3.88%
[±45]5 | 23.79 | 14.31 | 39.85%
The ultimate strength:
Linear degenaration
Experiment
Exponential degenaration | 
Simulation | Error
87.32 | 25.23%
50.67 | 7.35%
15.04 | 36.78%
Exponential degenaration
Former Results：

## Slide 16
Shear Nonlinearity：
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
刘魏光, 余音, 汪海. 考虑剪切非线性的复合材料渐进损伤模型[J]. 上海交通大学学报, 2016, 50(2):194-199.

## Slide 17
Experiment
Exponential degenaration
Results and Comparing
Displacement-Force curve of the [45/-45] 5 with different shape parameters.
linear

## Slide 18
Results and Comparing
n = 2 n = 3
experiment
shear nonlinearity:
The position of the initial failure is the same and argrees well with the experiment.

## Slide 19
Improvement
Failure mode with different Fracture energe ：
Refer to other papers:
Gm = 5 Gm = 0.5
A continuum damage model for composite laminates: Part II – Computational implementation and validation
Laminate damage model for composite structures

## Slide 20
CDM法与刚度折减法对比：
折减法 | CDM法
通过乘以折减系数使刚度矩阵退化，是一种半经验法的探索模型 | 基于不可逆过程的热力学，将势能定义为损伤变量的函数，损伤变量定义了应力应变的关系，同时取决于能量耗散值
折减系数的不确定 | 所有使用参数均可测量得到
不能模拟层合板的准脆性失效 | 可以模拟材料的弹脆性行为（无显著的塑形变形）
1 连续损伤模型（CDM法）