## Slide 1
Continumm damage model
Degeneration Model(linear vs exponential)
Shear Nonlinearity
Abaqus simulation
Characteristic Length
coefficient of viscosity
implicit dynamic
Results

## Slide 2
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1518 | 764.3 | 36.0 | 160.3 | 60
Table 2 Strength parameters of a single lamina
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 127.70 | 9.67 | 6.50 | 0.30
Table 1 Material properties of a single lamina
FEM：Abaqus
Model: 3D Shell(SC8R)
Strength criterion：Hashin
Simulation Model
Ф: 60mm, 80mm, 100mm
Layups: [0˚]10, [0˚/90˚]5, [±45˚]5

## Slide 3
calculate strain and undamaged stiffness matrix
calculate damage variable d and
calculate stress and Jacobian matrix; update damage variable d
damaged
undamaged
calculate damaged stiffness matrix
after each increment
quit UMAT,back to main program
calculate stress
UMAT subroutine
checkout failure ( Hashin
criterion)
UMAT subroutine：

## Slide 4
  Abaqus Simulation—Characteristic Length

## Slide 5
  Abaqus Simulation—coefficient of viscosity

## Slide 6
Prediction of size effects in notched laminates using continuum damage mechanics，P.P. Camanho a,*, P. Maimı´ b, C.G. Da´vila ,Composites Science and Technology 67 (2007) 2715–2727
The use of an implicit dynamic finite element model enables the prediction of the load drop that occurs when the specimens fail catastrophically.
implicit dynamic analysis VS static analysis
此处分析步的time period设为60，时间长度越大，越接近脆性。
将密度设为小值，保持不受惯性力的影响
  Abaqus Simulation—implicit dynamic

## Slide 7
Ultimate load （kN） Layer | Exp. | Linear degenaration | 
 |  | Simulation | Error
[0]10 | 69.73 | 86.98 | 24.73%
[0/90]5 | 47.20 | 45.37 | 3.88%
[±45]5 | 23.79 | 14.31 | 39.85%
The ultimate strength:
Linear degenaration
Experiment
Exponential degenaration | 
Simulation | Error
87.32 | 25.23%
50.67 | 7.35%
15.04 | 36.78%
Exponential degenaration
Former Results：

## Slide 8
Shear Nonlinearity：
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
刘魏光, 余音, 汪海. 考虑剪切非线性的复合材料渐进损伤模型[J]. 上海交通大学学报, 2016, 50(2):194-199.

## Slide 9
Experiment
Exponential degenaration
Results and Comparing
Displacement-Force curve of the [45/-45] 5 with different shape parameters.
linear

## Slide 10
Results and Comparing
n = 2 n = 3
experiment
shear nonlinearity:
The position of the initial failure is the same and argrees well with the experiment.

## Slide 11
Improvement
Failure mode with different Fracture energe ：
Refer to other papers:
Gm = 5 Gm = 0.5
A continuum damage model for composite laminates: Part II – Computational implementation and validation
Laminate damage model for composite structures