## Slide 1
Progressive damage analysis of Composite laminates with big cutouts
Chu PengCheng
2018.01.10

## Slide 2
Numerical Model
    Hashin Criteria & Continumm Damage Model(CDM)
    Ply-discount Method VS CDM
    Degeneration Model(linear vs exponential)
    Shear Nonlinearity
    in-situ strength effect
Abaqus Simulation
    Modeling Technique
    UMAT subroutine
    characteristic length
    coefficient of viscosity
    implicit dynamic
Overview：

## Slide 3
Strength | Xt | Xc | Yt | Yc | S12
(MPa) | 1518 | 764.3 | 36.0 | 160.3 | 60
Table 2 Strength parameters of a single lamina
ρ（kg/m3） | E1(GPa) | E2(GPa) | G12(GPa) | υ12
1520.7 | 127.70 | 9.67 | 6.50 | 0.30
Table 1 Material properties of a single lamina
FEM：Abaqus
Model: 3D Shell(SC8R)
Strength criterion：Hashin
Problem：
Ф: 60mm, 80mm, 100mm
Layups: [0˚]10, [0˚/90˚]5, [±45˚]5

## Slide 4
  Numerical Model
  Hashin criteria & Continuum Damage Model
Hashin criterion
Damage variable:
The Continuum Damage Model:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Damage constitutive matrix:

## Slide 5
  Numerical Model
  Degeneration Model(linear vs exponential)
Damage variable:
Lapczyk I, Hurtado J A. Progressive damage modeling in fiber-reinforced materials[J]. Composites Part A Applied Science & Manufacturing, 2007, 38(11):2333-2341.
Damage variable:
Damage and Failure Study of Composite Laminates with
Reinforced Cutout Based on CDM
Wang Wenzhi，Wan Xiaopeng，Yao Liaojun
Exponential degenaration:
Linear degenaration:
Maimí P, Camanho P P, Mayugo J A, et al. A continuum damage model for composite laminates: Part II – Computational implementation and validation[J]. Mechanics of Materials, 2007, 39(10):909–919.

## Slide 6
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
刘魏光, 余音, 汪海. 考虑剪切非线性的复合材料渐进损伤模型[J]. 上海交通大学学报, 2016, 50(2):194-199.
  Numerical Model
  ——Shear Nonlinearity

## Slide 7
  Numerical Model
  ——in-situ effect
在传统强度理论研究中，通常将单向板试验获得的拉伸、压缩和剪切强度值作为材料的固有属性并用于建立强度准则，进而预测多向层合板的强度。然而通过一系列试验研究发现，对于铺层方向和厚度都相同的子层，它在多向层合板内和在单向板内时表现出的基体强度（包括横向拉伸和剪切强度）不同，在层合板内表现的强度明显高于在单向板内，许多文献将层合板的这种现象称为就地效应（in-situ effect）。
李彪，李亚智，杨帆．考虑复合材料层合板就地效应的强度理论[J]．航空学报，2014，35(11)：3025-3036
By examining the results presented previously,5±7 we take the in-situ tensile transverse and shear strengths to be 1.5 times those measured from unidirectional laminates for all the laminates discussed.
Sun C T, Tao J. Prediction of failure envelopes and stress/strain behaviour of composite laminates 1[J]. Composites Science & Technology, 1998, 58(7):1125-1136.
为单层板的固有横向拉伸强度与固有面内剪切强度， 为单层板在层合板中相应的就低强度，ABCD为材料相关的常数，N为层合板中同一方向并相邻的单层板的层数。 是本单层的纤维铺设角度与其相邻的两个单层板纤维铺设角度之差。
Wang J, Karihaloo B L. Optimum In Situ Strength Design of Composite Laminates. Part I: In Situ Strength Parameters[J]. Journal of Composite Materials, 1996, 30(12):1314-1337.

## Slide 8
Results：
[0/90]5 | 60 |  |  | 80 |  |  | 100 |  | 
 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
Linear | 52.67 | 59.32 | 11.2% | 43.83 | 47.20 | 7.1% | 34.56 | 37.54 | 7.9%
Exponential | 56.72 |  | 4.4% | 48.17 |  | 2.1% | 34.59 |  | 7.9%
1、从试验以及模拟的结果来看，裂纹的扩展和孔径大小无关，孔径越小，极限载荷越大
2、计算结果可以表现出[0/90]5板的脆性断裂，
3、linear或是exponential模型对损伤演化的影响不太大，exponential比linear计算极限载荷的误差更小
[0/90]5
Ultimate loading：
Simulation
Experiment

## Slide 9
Results：
孔径 | 60 |  |  | 80 |  |  | 100 |  | 
[±45]5 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
Linear | 21.41 | 28.72 | 25.5% | 17.03 | 23.79 | 28.4% | 12.75 | 17.60 | 27.6%
Exponential | 27.34 |  | 4.8% | 21.73 |  | 8.7% | 16.09 |  | 8.6%
1、从试验以及模拟的结果来看，裂纹的扩展和孔径大小无关，孔径越小，极限载荷越大
2、linear或是exponential模型对损伤演化的影响不太大，极限载荷：exponential比linear误差更小
4、位移载荷曲线的形状和实验相差大
[±45]5
Ultimate loading：
Simulation
Experiment

## Slide 10
Results：
[±45]5
Shear Nonlinearity:
Problem:The load of the curve doesn't drop in the simulation result.
孔径 | 60 |  |  | 80 |  |  | 100 |  | 
[±45]5 | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error | Simul. | Exp. | Relative error
No shear nonlinearity | 27.34 | 28.72 | 4.8% | 21.73 | 23.79 | 8.7% | 16.09 | 17.60 | 8.6%
Shear nonlinearity | 26.81 |  | 6.7% | 21.39 |  | 10.1% | 16.01 |  | 9.0%
shear nonlinearity constitutive relations for the laminates were defined with the Ramberg-Osgood equation:
n is a parameter define the shape of the nonlinear stress-strain relationship.

## Slide 11
  Results：in-situ effect
材料参数 铺层 | 纤维拉伸强度Xt | 剪切强度Sxy | 基体拉伸强度Yt | 基体断裂能Gm
[0]10 | 970 | 63 | 36 | 0.5
[0/90]5 | 1455 | 95 | 54 | 2.5
[±45]5 | 1455 | 95 | 54 | 2.5
let A、B、C、D=1,we can obtain:
Sxy = 95;Gm = 5
[0]10
Sxy=63;Gm = 0.5
Sxy=63;Gm = 5

## Slide 12
Conclusions：
1、The simulation using the continuum damage model exhibit the brittle failure of the composite laminates as the experiment shows, it also preforms well for predicting the failure evolution behavior of composite laminates with big cutouts;
2、The exponential degeneration law performs better than linear degeneration law fro pridecting the ultimate strength in this simultion.
3、The shear nonlinearity must be considered for the [±45]5 layup laminates to obtain the displacement-force curve.
4、The in-situ effect should be considered,the strength should be calculated respectively for each layup of the laminates.
Future task：
1、paper and thesis
2、stress concentration factor
3、bulking and failure(optimize and design for composite laminates)
4、cohesive element